MORTAR MIXING GUIDE

Portland Cement + Lime + Mason Sand | Buckets, Shovels and Bag Conversions

MOST IMPORTANT: Mortar ratios are measured by VOLUME, not by equal bag weight. Use the same bucket or the same level shovel for every ingredient.

# 1. Standard Portland-Lime Mortar Ratios

| Type | Portland cement | Hydrated lime | Mason sand | Typical use / minimum strength |
| --- | --- | --- | --- | --- |
| M | 1 part | 1/4 part | 3 3/4 parts | Heavy loads, foundations, retaining walls ¦ 2,500 psi |
| S | 1 part | 1/2 part | 3 1/2-4 1/2 parts | Exterior structural masonry, steps, below grade ¦ 1,800 psi |
| N | 1 part | 1 part | 6 parts | Above-grade brick, veneer and general work ¦ 750 psi |
| O | 1 part | 2 parts | 9 parts | Soft/older masonry and protected interior work ¦ about 350 psi |

# 2. Easy Whole-Number Bucket Batches

| Type | Portland buckets | Lime buckets | Sand buckets | Total dry parts |
| --- | --- | --- | --- | --- |
| M | 4 | 1 | 15 | 20 |
| S | 2 | 1 | 7-9 | 10-12 |
| N | 1 | 1 | 6 | 8 |
| O | 1 | 2 | 9 | 12 |

TYPE S JOBSITE DEFAULT: For the stronger end of Type S, use 2 buckets Portland + 1 bucket lime + 9 buckets mason sand. For every batch, keep the measuring bucket consistent.

# 3. Shovel Batches

| Type | Small shovel recipe | Larger batch if 3 level shovels fill your bucket |
| --- | --- | --- |
| M | 4 Portland + 1 lime + 15 sand | 12 Portland + 3 lime + 45 sand |
| S | 2 Portland + 1 lime + 7-9 sand | 6 Portland + 3 lime + 21-27 sand |
| N | 1 Portland + 1 lime + 6 sand | 3 Portland + 3 lime + 18 sand |
| O | 1 Portland + 2 lime + 9 sand | 3 Portland + 6 lime + 27 sand |

CALIBRATE YOUR SHOVEL: Fill one 5-gallon bucket using your normal LEVEL shovels and count them. A shovel is not a fixed unit; shovel size and how high it is heaped can change the mix.

# 4. Sand Bags: Pounds, Cubic Feet and Correct Conversions

Bag weight alone is not a reliable volume measurement. Read the bag's stated yield. One manufacturer's mason sand lists the following approximate dry volumes:

| Mason sand bag | Published approximate volume | 5-gallon bucket equivalent |
| --- | --- | --- |
| 50 lb | 0.60 cubic foot | about 0.90 bucket |
| 80 lb | 0.80 cubic foot | about 1.20 buckets |

## What Does One Full 5-Gallon Bucket Weigh?

A level 5-gallon bucket holds 0.668 cubic foot. The weights below are practical estimates, not fixed laws. Material brand, packing, moisture and how full the bucket is can change the reading.

| Material | Approx. loose density | Approx. weight in one LEVEL 5-gal bucket | Best practice |
| --- | --- | --- | --- |
| Plain Portland cement | 94 lb/ft3 | about 63 lb | Use volume for ratios; a 94-lb bag is about 1.50 buckets. |
| Dry mason sand | about 83-100 lb/ft3 | about 56-67 lb | Weigh your own bucket because sand and moisture vary. |
| Type S hydrated lime | about 40-50 lb/ft3 | about 27-33 lb | Fluff/packing changes volume; avoid compacting it. |
| Water | 62.4 lb/ft3 | about 41.7 lb (5 gallons) | Do not use a full bucket automatically; add gradually. |

NO-CONFUSION RULE: For accurate field work, mark a fill line on one bucket. Fill it with your actual sand, weigh the full bucket, subtract the empty bucket weight, and write that net sand weight on the bucket.

## One 94-lb Bag of Plain Portland Cement

A 94-lb Portland cement bag is approximately 1 cubic foot, or about 1.50 five-gallon buckets. The sand counts below use the published 0.60 ft3 yield for a 50-lb sand bag and 0.80 ft3 for an 80-lb sand bag.

| Type | Sand volume | Approx. 50-lb sand bags | Approx. 80-lb sand bags | Hydrated lime volume |
| --- | --- | --- | --- | --- |
| M | 3.75 ft3 | 6.25 bags | 4.69 bags | 0.25 ft3 |
| S | 3.5-4.5 ft3 | 5.83-7.50 bags | 4.38-5.63 bags | 0.50 ft3 |
| N | 6.00 ft3 | 10.00 bags | 7.50 bags | 1.00 ft3 |
| O | 9.00 ft3 | 15.00 bags | 11.25 bags | 2.00 ft3 |

## One 47-lb Bag of Plain Portland Cement

A 47-lb bag is approximately 0.50 cubic foot, or about 0.75 of a five-gallon bucket. This is exactly half of the 94-lb-bag batch.

| Type | Sand volume | Approx. 50-lb sand bags | Approx. 80-lb sand bags | Hydrated lime volume |
| --- | --- | --- | --- | --- |
| M | 1.875 ft3 | 3.13 bags | 2.34 bags | 0.125 ft3 |
| S | 1.75-2.25 ft3 | 2.92-3.75 bags | 2.19-2.81 bags | 0.25 ft3 |
| N | 3.00 ft3 | 5.00 bags | 3.75 bags | 0.50 ft3 |
| O | 4.50 ft3 | 7.50 bags | 5.63 bags | 1.00 ft3 |

## One Full 5-Gallon Bucket of Portland: Material Weights

| Type | Portland | Lime buckets / approx. lb | Sand buckets | Approx. dry sand weight |
| --- | --- | --- | --- | --- |
| M | 1 bucket / ~63 lb | 1/4 bucket / ~7-8 lb | 3 3/4 | about 210-251 lb |
| S | 1 bucket / ~63 lb | 1/2 bucket / ~13-17 lb | 3 1/2-4 1/2 | about 196-302 lb |
| N | 1 bucket / ~63 lb | 1 bucket / ~27-33 lb | 6 | about 336-402 lb |
| O | 1 bucket / ~63 lb | 2 buckets / ~54-66 lb | 9 | about 504-603 lb |

## Sand Bags per One Full 5-Gallon Bucket of Portland

| Type | 50-lb sand bags (0.60 ft3 each) | 80-lb sand bags (0.80 ft3 each) | Lime needed |
| --- | --- | --- | --- |
| M | about 4.18 bags | about 3.13 bags | 1/4 bucket |
| S | about 3.90-5.01 bags | about 2.92-3.76 bags | 1/2 bucket |
| N | about 6.68 bags | about 5.01 bags | 1 bucket |
| O | about 10.03 bags | about 7.52 bags | 2 buckets |

BUYING TIP: Round material UP and allow roughly 10% for waste. Sand moisture, compaction and brand-specific bag yield can change the real volume.

# Is One Shovel of Portland Good for Three Sand Bags?

NO - NOT FOR NORMAL MORTAR: Three 50-lb mason-sand bags equal about 1.8 ft3 of sand. A Type S ratio needs about 0.40-0.51 ft3 of Portland cement (roughly 38-48 lb) plus about 0.20-0.26 ft3 of hydrated lime. One ordinary shovel of Portland is far too little and would create a weak, sandy mix.

What the person may have meant:

| Possible statement | What it actually means |
| --- | --- |
| 1 bag masonry cement + 3 sand | Usually 1 part masonry cement to 3 parts mason sand BY VOLUME; follow that exact bag label. |
| 1 bag masonry cement + about 3 ft3 sand | A common field batch for certain bagged masonry cements - not one shovel of Portland. |
| 1 Portland + 3 sand | Could mean 1 bucket Portland to 3 buckets sand, but lime and the specified mortar type still matter. |

# 5. Know What Bag You Bought

| Words printed on bag | Usually add | Do not assume |
| --- | --- | --- |
| Portland Cement | Hydrated lime + mason sand + water | It is not complete mortar. |
| Type S / N Masonry Cement | Mason sand + water per label | Do not automatically add Portland or lime. |
| Type S / N Mortar Mix | Water only | It normally already contains sand. |
| Concrete Mix | Water only | Contains gravel; not brick-joint mortar. |
| Sand Mix / Topping Mix | Water, or additions specifically approved | Not automatically a substitute for masonry mortar. |

# 6. Which Mortar Should I Use?

| Application | Common starting point | Important caution |
| --- | --- | --- |
| Newer exterior brick/block above grade | Type N or specified mortar | Match unit strength and plans; stronger is not always better. |
| Load-bearing / below-grade / retaining wall | Type S or engineered specification | Drainage, reinforcement and code design still matter. |
| Heavy foundation or high-load masonry | Type M when specified | Very hard mortar can damage softer masonry. |
| Repointing older soft brick | Compatible softer restoration mortar | Test/match existing mortar; avoid blindly using Type S or M. |
| Parging / stucco | Use the specified stucco/parge system | Coat recipes differ from brick-laying mortar. |
| Concrete slab, footing or thick step | Concrete mix with stone aggregate | Mortar is not a substitute for structural concrete. |

## Detailed Mortar-Type Guide

| Type | Workability / hardness | Good candidates | Avoid or verify first |
| --- | --- | --- | --- |
| M | Hardest; least flexible of these common types | High-load and below-grade masonry when specified | Soft brick, ordinary repointing, historic walls |
| S | High strength with moderate flexibility | Structural exterior masonry, retaining/foundation work | Historic soft brick; thin cosmetic patches without proper system |
| N | Medium strength; better movement accommodation | Most above-grade modern brick/veneer and general masonry | Below-grade or heavily loaded work unless designed |
| O | Low strength; softer and more flexible | Protected work and some older/softer masonry | Structural, exposed, below-grade or high-load work |
| K / lime-rich | Very soft; specialty restoration formulation | Certain very old historic masonry after analysis/specification | Do not field-invent; use preservation professional/spec |

TYPE N REMINDER: Type N is not 'bad' or automatically too weak. Its softer, more workable character is often appropriate for above-grade brick and general repointing when it is compatible with the masonry. Type S is stronger, but stronger is not always safer for the brick.

# 7. Water and Mixing Procedure

| Step | Action | Field check |
| --- | --- | --- |
| 1 | Measure dry materials | Use identical buckets or level shovels. Never switch measuring methods halfway through a batch. |
| 2 | Dry blend | Mix Portland cement, hydrated lime and sand until the color is uniform. |
| 3 | Add clean water slowly | There is no universal water amount for field-batched mortar because sand moisture changes daily. |
| 4 | Mix thoroughly | Mechanical mixing is preferred. Mix until uniform and workable; scrape dry material from the mixer sides. |
| 5 | Check consistency | Mortar should cling to the trowel, spread cleanly and hold a ridge without flowing like soup. |
| 6 | Use consistently | Keep every batch's material source, ratio, water and mixing time consistent to reduce color variation. |

WATER WARNING: Too much water increases shrinkage, lowers strength, encourages cracking and changes mortar color. Add water in small amounts. Never pour in an unmeasured large amount just to make the mix easier.

# 8. Jobsite Quality Checklist

| Stage | Check |
| --- | --- |
| Before mixing | Confirm mortar type, inspect bag labels, use clean mason sand, clean water and clean tools. |
| During mixing | Keep ratios consistent; record bucket/shovel counts; avoid heaped, inconsistent shovels. |
| Before placing | Remove dust and loose material; prepare/dampen masonry only as appropriate for the unit and conditions. |
| During installation | Keep joint depth and tooling timing consistent. Do not smear overly wet mortar across brick faces. |
| Weather | Follow cold- and hot-weather masonry rules. Protect fresh work from freezing, heavy rain, rapid drying and direct heat. |
| Historic work | Match mortar composition, hardness, color and aggregate. Use a mortar analysis/specification when necessary. |

# 9. Common Mistakes to Avoid

| Mistake | Why it causes problems |
| --- | --- |
| Using equal pounds as equal parts | Mortar proportions are based on volume; materials have different densities. |
| Adding sand to premixed mortar | The bag already contains sand; extra sand can seriously reduce strength. |
| Using straight Portland and sand for brick | Poor workability and water retention; lack of lime/mortar system can reduce bond. |
| Choosing the strongest mortar automatically | Mortar harder than the brick can transfer stress and contribute to brick spalling. |
| Guessing with wet, heaped shovels | Every batch changes, causing inconsistent strength, workability and color. |

# 10. Bucket Calibration Record

| Measurement | Record your jobsite value |
| --- | --- |
| Empty 5-gallon bucket weight | __________ lb |
| Bucket + level dry sand | __________ lb |
| Net dry sand weight (subtract empty bucket) | __________ lb |
| Number of your level shovels per bucket | __________ shovels |
| Sand brand / bag size / date | ____________________________________________ |

MOISTURE CHECK: Wet sand can weigh substantially more while occupying approximately the same measured bucket volume. Mortar recipes stay volume-based. Do not add extra Portland merely because the wet sand bucket weighs more.

# 11. Batch Record

| Job / date | Mortar type | Portland measure | Lime measure | Sand measure | Notes |
| --- | --- | --- | --- | --- | --- |
| ____________ | _____ | ____________ | ____________ | ____________ | ________________ |
| ____________ | _____ | ____________ | ____________ | ____________ | ________________ |
| ____________ | _____ | ____________ | ____________ | ____________ | ________________ |

# 12. Safety and Storage

| Hazard / issue | Jobsite control |
| --- | --- |
| Cement and lime burns | Wear alkali-resistant gloves, long sleeves and eye protection. Wash exposed skin promptly; do not kneel in wet mortar. |
| Silica dust from sand/mixing | Avoid dry sweeping and uncontrolled dust. Use suitable dust controls and a properly selected respirator when required by the task/exposure plan. |
| Eye exposure | Use sealed eye protection while dumping and dry mixing. Flush with clean water immediately and obtain medical help as directed by the SDS. |
| Bag storage | Keep Portland, lime and premixed mortar dry, elevated and covered. Discard material that has hardened into moisture-damaged lumps. |
| Weather | Protect fresh mortar from freezing, heavy rain, high wind and rapid drying. Follow project and code hot-/cold-weather requirements. |

# Sources and Field Disclaimer

Reference basis: QUIKRETE Portland Cement and Masonry Cement manufacturer mixing guidance; Sakrete Mason Sand published bag yields; ASTM C270-related mortar classifications and minimum compressive strengths as summarized by established manufacturers. Always follow the project drawings, local code, engineer/architect specifications, historic-preservation requirements and the exact product label. This field guide does not replace a project-specific mortar specification or laboratory mortar analysis.