HAMMER BRICK & HOME LLC

Masonry Mortar Matching & Tune-Up Guide

---------------------------------------

1. PURPOSE

A complete field guide for matching old mortar, mixing correctly, and applying professional-grade masonry tune-up work for NYC homes.

2. HOW TO MATCH OLD MORTAR (FULL STEPS)

A. Identify Existing Mortar Type

- Type N: Common for facades, walkways, and general joints. Softer and flexible.

- Type S: Stronger, used for steps, high-traffic areas, structural edges.

- Lime Mortar: Found in older brownstones; lighter color, softer texture.

Scratch Test:

- Scratches easily → Type N or lime.

- Very hard → Type S.

B. Take a Sample

- Remove a pea-sized piece of old mortar.

- Bring to a masonry supply store for sand match & color analysis.

C. Match the Sand (Most Important)

- 90% of color comes from sand.

- Check sand grain size and color.

- Use similar sand from masonry supply, not Home Depot generic sand.

D. Base Mortar

- Use Type N for walls and brick joints.

- Use Type S for steps, walkways, structural repairs.

- Never use Type S on old soft brick.

E. Pigment Adjustment

- Start with no pigment.

- Add charcoal pigment in tiny amounts only if needed.

- Test dry samples before final mixing.

F. Test Samples

- Apply a sample to cardboard.

- Let dry 20–30 min.

- Compare in daylight.

- Adjust pigment or sand ratios as needed.

G. Water Ratio

- Peanut butter consistency.

- Not soupy.

- Not dry.

- Mix → rest 5 minutes → mix again (slake).

H. Tooling

- Match original joint finish: concave, flush, V-joint, raked, struck, weathered.

- Light brushing after partial set.

I. Final Cure

- Mist lightly to slow the cure.

- No acid wash.

- Brush haze after 24 hours.

---------------------------------------

3. 90% FORMULA (NYC STANDARD MATCH RECIPE)

This formula matches MOST NYC homes (90% accuracy).

RECIPE:

- Type N mortar mix (base)

- 50% tan sand

- 50% white masonry sand

- 1/4 teaspoon charcoal pigment per quart of mortar

- Water to peanut-butter consistency

BEST FOR:

- Stoops

- Walkways

- Steps

- Facade touch-ups

---------------------------------------

4. WHERE TO BUY MATERIALS

A. Masonry Supply Stores (Best Match)

- Staten Island Masonry Supply

- Brooklyn Sand & Stone

- Liberty Building Supply

- Kuiken Brothers (NJ)

They provide exact sand matching.

B. Home Depot (General Use)

- Type N / Type S mortars

- Mortar pigments (charcoal)

- Bonding agents

- Basic masonry tools

C. Specialized Lime Mortar

- U.S. Heritage Lime Mortar

- LimeWorks.us

---------------------------------------

5. HOW TO MIX MORTAR (FIELD PROCEDURE)

STEP 1 — Bucket Setup

- Use a clean bucket.

- Add sand first.

- Add mortar second.

STEP 2 — Water Addition

- Add water slowly.

- Mix until peanut butter consistency.

- Let sit 5 minutes.

- Mix again.

STEP 3 — Test a Small Amount

- Apply small dab.

- Let dry 20 minutes.

- Compare color to old mortar.

STEP 4 — Adjust

- Too light? Add small charcoal pigment.

- Too dark? Add more white sand.

- Too gray? Add tan sand.

- Too yellow? Reduce tan sand.

STEP 5 — Apply in Joints

- Fill with pointing trowel.

- Compact mortar tightly.

- Finish with matching joint tool.

STEP 6 — Final Cure

- Keep shaded from sun.

- Mist gently.

- Avoid freezing conditions.

---------------------------------------

6. SAFETY RULES

- Wear gloves (alkaline material).

- Use eye protection when grinding.

- Use dust mask when removing old mortar.

- Keep bonding agent off skin.

- Clean tools immediately after use.

---------------------------------------

7. QUICK CHECKLIST FOR MASONRY TUNE-UP SPECIAL

- Repoint 6–8 joints

- Fill cracks

- Blend mortar color with existing

- Tool joints to match original style

- Surface cleanup

- Safety check for trip hazards

- Photos for before/after

---------------------------------------

END OF DOCUMENT