# NYC DOT Sidewalk Repair Field Guide
(For Contractors – First Job Cheat Sheet)

## 1. Overview & Disclaimer

This guide is to help you, as a home improvement / masonry contractor, repair a NYC sidewalk that has a Department of Transportation (DOT) violation. It is a practical field guide, not legal advice. Always check the latest NYC DOT rules, permits, and specifications before starting work.

Key goals of a compliant repair:

- Remove trip hazards and unsafe conditions.

- Use DOT-acceptable concrete mix from an approved plant.

- Build proper base and slab thickness.

- Set correct slope so water drains to the curb (no ponding).

- Use proper joint spacing, expansion material, and finishes.

- Protect city trees and utilities.

- Provide clean documentation to the property owner so they can request DOT to close the violation.

## 2. Why DOT Issues Sidewalk Violations

Common reasons DOT writes a sidewalk violation on a property:

- Trip hazards – vertical difference of about 1/2" or more between flags.

- Broken, cracked, or heaving slabs – pieces loose or rocking.

- Spalling or surface deterioration – holes or pits 1/2" deep and 1" or more in diameter.

- Ponding water – slab is low or back-pitched and holds water instead of draining to the curb.

- Tree root lifting – sidewalk raised significantly by tree roots.

- Obstructions – dangerous slopes, missing flags, large gaps.

The owner is responsible for fixing the sidewalk. You repair the sidewalk; the owner later submits proof to DOT to close the violation.

## 3. Licensing, Insurance & Permits (Contractor Requirements)

Before working on NYC sidewalks, make sure you are properly set up:

- NYC Home Improvement Contractor (HIC) License (if doing residential work).

- General Liability Insurance with appropriate limits and correct description of operations.

- Workers’ Compensation and Disability/DBL if you have employees.

- DOT Sidewalk/Street Opening or Sidewalk Repair Permit where required.

- If you will occupy the road or curb lane, a DOT occupancy permit and any required traffic control plan.

Always call 811 (utility mark-out) before you dig or break out slabs. Hitting a gas or electric line can be deadly and extremely expensive.

## 4. Concrete Mix Requirements (What to Order)

NYC sidewalks must be constructed with standard DOT sidewalk concrete from an approved plant. When you order concrete, tell the plant clearly what you need.

When ordering, say something like:

"NYC DOT standard sidewalk mix, 3,200–4,000 PSI, air-entrained, from a DOT-approved plant."

Typical characteristics of a compliant sidewalk mix:

- Compressive strength: approximately 3,200–4,000 PSI at 28 days.

- Single-course slab (no separate topping) – the whole thickness is one pour.

- Air-entrained concrete to resist freeze–thaw.

- Slump usually around 3–4" (ask the plant). Avoid adding excess water on site.

Do not allow helpers to flood the mix with water in the wheelbarrow – this weakens the concrete, increases shrinkage cracking, and may cause surface damage.

## 5. Thickness & Base Requirements

Different locations require different slab thicknesses, but a properly prepared base is always critical.

Typical NYC requirements:

| Location | Concrete Thickness | Base (Subbase) |
| --- | --- | --- |
| Standard sidewalk (no driveway load) | 4" concrete slab | 6" compacted crushed-stone base (Item 4 or similar) |
| Driveway apron / where vehicles cross | 7" concrete slab | 6" compacted crushed-stone base |

Base preparation best practices:

- Remove all old concrete, loose soil, organic material, garbage, roots, and soft spots.

- Install a granular base (crushed stone, Item 4, or similar), not random fill or topsoil.

- Compact base in lifts with a plate compactor until it is firm and shaped to the correct pitch.

- Base should already follow the slope you want in the finished slab (toward the curb).

## 6. Sidewalk Layout & Flag Sizes

NYC standard practice is to divide the sidewalk into concrete “flags” (panels) using score joints.

General layout rules:

- Standard flag size is about 5' x 5' where feasible.

- Frontage is usually divided into 5' sections from the property line; any odd-sized flag is placed closest to the building or property line.

- Score joints should form a clean, straight grid, aligned with existing neighboring flags.

- Avoid creating very narrow strips (less than 2–3 feet) if possible.

## 7. Joints: Contraction & Expansion

Proper jointing controls cracking and allows for movement between slabs, buildings, and curbs.

A. Contraction / score joints (dummy joints):

- These create the 5' x 5' pattern and help control where cracks occur.

- They are usually spaced about 5' apart in each direction.

- They should be tooled or sawed to a depth of about 1/4 of the slab thickness (around 1" in a 4" slab).

- Lines must be straight and should line up with joints in adjoining sidewalk slabs.

B. Expansion joints (with filler material):

- Used where the sidewalk meets rigid structures such as building walls, curbs, or other fixed objects.

- Also generally placed at intervals along long runs (for example, every 20 feet) to allow expansion and contraction.

- Constructed with pre-molded expansion joint filler (often 1/2" thick), full depth of the concrete slab.

- Top of filler is typically set slightly below the surface and sealed with joint sealer if required.

- Expansion joints help prevent the slab from pushing against structures and cracking.

## 8. Slope / Pitch Requirements

Correct slope is essential to prevent ponding water and to meet accessibility (ADA-style) standards.

A. Transverse slope (from building toward curb):

- Sidewalk must slope from the property side toward the curb so water drains off the slab.

- Typical safe target is around 2% cross slope – about 1 to 1-1/4" of drop across a 5' sidewalk (approximately 1/4" per foot).

- Too little slope can cause ponding; too much slope can be difficult for pedestrians and may not be ADA-friendly.

B. Longitudinal slope (along the length of the sidewalk):

- Follow the grade of the existing curb and street.

- Avoid creating humps or sags that trap water.

- If the street itself is poorly graded, do the best you can to keep a uniform, walkable slope.

Use a level and tape measure to check slopes while setting forms. Do not rely only on eye – a small pitch error can create water problems.

## 9. Surface Finish (Texture & Appearance)

DOT expects a non-slip, even, and professional finish.

Basic finishing steps:

- After placing concrete, strike off (screed) to proper level using straightedges aligned with forms.

- Bull float to embed aggregate and smooth the surface without overworking.

- Allow bleed water to evaporate before final finishing – do not trowel while bleed water is present.

- Tool the edges and joints with an edger and jointer for a clean appearance.

- Apply a medium broom finish across the slab (usually perpendicular to the direction of travel) for slip resistance.

- Avoid hard steel-trowel finishes that can become slippery when wet.

Final surface should be free of major ridges, depressions, honeycombing, and footprints. Small hairline cracks are normal; large or random cracks can be an issue.

## 10. Trees, Tree Roots & Tree Pits

Street trees often cause sidewalk damage. NYC is very protective of street trees, and you must be careful when working near them.

Key points around trees:

- Do not cut major tree roots without checking local rules and, if needed, contacting the Parks Department.

- Never bury the tree trunk flare under concrete.

- Maintain or create a proper tree pit (open soil area) around the tree, sized according to local standards.

- Use flexible design solutions (shorter flags, ramping between flags, or special details) approved by the city when roots make standard slopes impossible.

## 11. Utilities & Underground Conditions

Before breaking concrete, always assume that utilities may be underneath the sidewalk.

Important steps:

- Call 811 and wait for utility mark-outs before digging or jackhammering.

- Hand dig carefully where marks indicate gas, electric, or other utilities.

- If you expose a utility or damage one, stop work immediately and follow emergency procedures.

## 12. Step-by-Step: Replacing a Sidewalk Flag to DOT Standards

Use this as a job checklist:

1. Review the violation notice and inspect the entire sidewalk. Decide which flags must be replaced.

2. Confirm licensing, insurance, and any required DOT permits. Call 811 for utility mark-outs.

3. Take clear before photos of all damaged areas from multiple angles for your records and for the owner.

4. Snap chalk lines to match existing joint layout and standard 5' x 5' flags. Mark full-depth sawcut lines.

5. Sawcut around the flag(s) to be removed, full depth. Protect adjacent slabs from damage.

6. Break out and remove the entire flag(s), including any loose pieces. Dispose of debris properly.

7. Excavate subgrade to provide room for about 6" of compacted stone base plus the required concrete thickness (4" or 7").

8. Install and compact the crushed stone base, shaping it to the correct cross-slope and longitudinal slope.

9. Set forms at the proper elevation so the finished slab will match adjacent flags and pitch correctly toward the curb.

10. Install expansion joint filler where the new slab meets building walls, existing slabs (where required), curbs, or other structures.

11. Re-check slopes with a level and tape measure (target around 1/4" per foot cross slope toward the curb).

12. Order DOT-approved sidewalk concrete and be ready with crew, tools, and access before the truck arrives.

13. Place concrete, consolidate it, strike off, bull float, and install contraction (score) joints in a 5' x 5' pattern aligned with surrounding sidewalk.

14. Edge all slab edges and joints, then apply a medium broom finish for slip resistance.

15. Protect the fresh concrete with barriers, caution tape, and/or cones. Keep pedestrians off until it has set (at least 24 hours; longer in cold weather).

16. Do not allow vehicles on standard 4" sidewalk slabs. For 7" driveway slabs, keep vehicles off for several days until strength develops.

17. After curing, remove forms, backfill edges, and clean the work area.

18. Take clear after photos from the same angles as the before photos.

19. Provide the owner with your invoice, permit number(s), before/after photos, and any material tickets. Explain that they must contact DOT to request closing the violation.

## 13. Documentation Package for the Property Owner

When the job is complete, make it easy for the owner to get the violation closed by giving them a clean package of documentation.

Include:

- Copy of your contract or work order.

- Invoice showing sidewalk repair, address, and date.

- Permit numbers and copies of any DOT permits (if applicable).

- Concrete delivery tickets showing DOT mix and plant information.

- Before and after photos of all repaired areas.

- Your full business information: company name, address, phone, license number, and insurance (if requested).

Tell the owner they must submit a request to DOT (online or by mail, per current rules) with this documentation so DOT can inspect and close the violation.

## 14. Safety & Site Control

Safety is critical for your crew and the public.

Minimum safety practices:

- Wear appropriate PPE: hard hats, safety glasses, gloves, hearing protection, and work boots.

- Use high-visibility vests when working near traffic.

- Set up barricades, cones, and caution tape to keep pedestrians out of the work area.

- Provide safe alternate paths if you are blocking a major walkway.

- Secure tools and materials so they do not create trip hazards.

- Follow all DOT and OSHA rules for working in or near the roadway.

## 15. Final Notes & Best Practices

A few extra tips to protect yourself on your first sidewalk violation job:

- Walk the whole sidewalk with the owner and clearly explain which areas you will repair.

- Write a simple but clear scope of work that mentions thickness, base, and number of flags.

- Take more photos than you think you need – they protect you later if there are questions.

- Do not patch small sections of a cracked flag; replace the entire flag to meet DOT expectations.

- Keep the jobsite neat and respectful – neighbors and inspectors notice professionalism.

- If something on site conflicts with these general guidelines, check current NYC DOT published standards or call DOT for clarification.

This document is meant as a working field guide. Always verify the latest NYC DOT requirements, and when in doubt, build to a high standard of safety, drainage, and durability.