# Brownstone & Limestone Restoration – Complete Master Training Manual

Hammer Brick & Home LLC – Internal Professional Guide

# 1. SAFETY & BASIC KNOWLEDGE

- Brownstone is soft, porous, absorbs water fast.

- NEVER use concrete or waterproof paints.

- Goal: stability, breathability, texture match.

Safety Gear:

• Safety glasses

• N95 respirator

• Gloves

• Hearing protection

• Fall protection

📸 PHOTO 1 [Insert]

# 2. FULL TOOLS & MATERIALS LIST

Hand Tools:

• Chisels (½,1,1½)

• Mason hammer

• Margin & pointing trowels

• Flex putty knives

• Hard/soft wire brushes

• Sponges

• Buckets/mixing pails

Power Tools:

• Angle grinder

• Tuckpoint blade

• Grinding wheel

Materials:

• Jahn / Cathedral Stone / Prosoco repair mortars

• Bonding agent

• Breathable siloxane sealer

• Masking tape & plastic

📸 PHOTO 2 & 3 [Insert]

# 3. FACE PATCH – EXTREME DETAIL

STEP 1 — Inspection:

• Identify hollow, flaking, delaminated areas.

• Tap test.

• Outline 2 inches outside damaged zone.

📸 PHOTO 4

STEP 2 — Removal:

• Hold chisel 30–45°.

• Tap lightly.

• Remove only rotten stone.

📸 PHOTO 5 & 6

STEP 3 — Cleaning:

• Hard brush → soft brush.

• Mist to SSD condition.

📸 PHOTO 7 & 8

STEP 4 — Bonding Agent:

• Thin, even coat.

• No puddles.

📸 PHOTO 9

STEP 5 — Mixing Mortar:

• Water first.

• Peanut‑butter consistency.

• Slake 5 min.

📸 PHOTO 10

STEP 6 — Packing:

• Fill deep areas first.

• Thin lifts ¼–½".

• Compact well.

📸 PHOTO 11

STEP 7 — Shaping:

• Match existing geometry.

• Slight overbuild.

📸 PHOTO 12 & 13

STEP 8 — Texture:

• Sponge: sandy.

• Brush: grain.

• Knife: smooth.

📸 PHOTO 14

STEP 9 — Curing:

• Protect 24–72 hr.

• Mist lightly.

📸 PHOTO 15

FINISHED PATCH:

📸 PHOTO 16 & 17

# 4. LINTEL REPAIR – FULL DETAIL

STEP 1 — Identify cracking & rust.

STEP 2 — Remove loose stone carefully.

STEP 3 — Clean & treat rust.

STEP 4 — Bond, pack mortar, recreate edge.

📸 PHOTO 18–22

# 5. SILL NOSE & CORNER REPAIR – FULL DETAIL

• Chip loose underside.

• Clean → dampen → bond.

• Use straight edge to form nose.

• Shape corners with pointing trowel.

📸 PHOTO 23–26

# 6. WATERPROOFING & SEALING – COMPLETE

• Only use breathable siloxane/silane.

• Apply evenly with sprayer/brush.

• Avoid glossy sealing.

📸 PHOTO 27–29

# 7. PRACTICE & TRAINING PROGRAM

• Patch boards practice.

• First real job on low visibility.

• Review texture, edges, blend.

📸 PHOTO 30

# 8. JOBSITE CHECKLIST VERSION

• PPE on

• Inspect → outline

• Remove loose stone

• Clean SSD condition

• Bond coat applied

• Mortar mixed & slaked

• Packed in thin lifts

• Shaped & textured

• Protected for cure

# 9. CUSTOMER‑FRIENDLY PDF CONTENT

• What is brownstone?

• Why does it fail?

• How repairs work

• Before/after examples

• Warranty explanation

• Maintenance schedule

# 10. PRICING & SCOPING GUIDE

Small Patch: 3x3" – 6x6"

Medium Patch: 6x6" – 12x12"

Large Patch: Full sill/step sections

Add-ons:

• Color matching

• Waterproofing

• Crack stitching

• Lintel edge rebuild

# 11. COMMON MISTAKES & FIXES

Mistake: Overworking mortar → smooth finish.

Fix: Re-texture with sponge/brush.

Mistake: Patching over wet surface.

Fix: SSD only.

Mistake: Using concrete.

Fix: Always stone repair mortars.

Mistake: Not removing enough loose stone.

Fix: Expand cavity until solid.